Policarbonato - P.C.

Chemical	Polycarbonate

Designation:

DIN Abbreviation:	PC

Colour, Filler:	Transparent

Stock Availability:	Standard length 3 metres, also cut to size

( Rod 	4  -   250 mm dia

( Plate	1  -   100 mm thick

( Tube	up to 200 mm OD

( Profile

( Finished parts, machined or injection moulded

Policarbonato P;C.  is an amorphous engineering thermoplastic with high transparency and toughness for varied applications.

Main characteristics:	( transparent	( easily machined and polished,

( very tough	  care required with coolant,

( strong	  susceptible to stress cracking

( good heat deformation		( easily welded

resistance	 	( easily bonded

( good electrical insulation

Preferred Fields:	Mechanical engineering, model making, automotive engineering, transport and conveyor technology, electrical engineering, precision engineering, household appliances, food technology, medical technology, photo technology, buildings

Applications:	( transparent working models	( housing parts

( insulators		( plugs

( plug strips		( sight glasses

( masking covers		( optical components

( photo couplers		( weather protection parts

Policarbonato - P.C.

The following information corresponds with our current knowledge and indicates our products and possible applications. We cannot give a legally binding guarantee of certain properties or the suitability for a specific application. Existing commercial patents must be observed. A definitive quality guarantee is given in our general conditions of sales. Unless otherwise stated, these values represent averages taken from injection moulding samples. We reserve the right of technical alterations.

Properties

|  | Unit | Test method DIN ASTM |
| --- | --- | --- |

| Mechanical |
| --- |
|  | Density | g/cm³ | 53 479 | 1.20 |
| Tensile strength at yield | MPa | 53 455 | 65 |
| Tensile strength at break | MPa | 53 455 |
|  | Elongation at break | % | 53 455 | 60 - 100 |
| Modulus of elasticity in tension | MPa | 53 457 | 2200 |
| Modulus of elasticity in flexure | MPa | 53 457 |
|  | Ball indentation hardness | MPa | 53 456 | 100 |
| Impact strength (Charpy) | kJ/m2 | 53 453 | no br. |
| Creep rupture strength after 1000 hrs with static load | MPa |
| 48 |
| Time yield limit for 1% elongation after 1000 hrs. | MPa |
| 18 |
| Coefficient of friction against hardened and ground steel p = 0,05 N/mm², v = 0,6 m/s | – |
| 0.52 - 0.58 |
| Wear conditions as above | µm/km |
| 22 |
| Thermal |
|  | Crystalline melting point | °C | 53 736 |

Glass transition temperature

|  | °C | 53 736 | 145 |
| --- | --- | --- | --- |

Heat distortion temperature Method A                        Method B

|  | °C °C | ISO 75 ISO 75 | 135 140 |
| --- | --- | --- | --- |

| Properties | Unit | Test method DIN ASTM |
| --- | --- | --- |

| Thermal |
| --- |
|  | Max. service temperature short term long term | °C °C |
| 140 120 |
| Coefficient of thermal conductivity | W/(m . K) |
| 0.19 |
| Specific heat | J/(g . K) |
| 1.2 |
| Coefficient of thermal expansion | 10-5/K |
| 6 - 7 |
| Electrical |
|  | Dielectric constant at 105 Hz |
| 53 483 | 3 |
| Dielectric loss factor at 105 Hz |
| 53 483 | 0.006 |
| Specific volume resistance | ( . cm | 53 482 | 1017 |
| Surface resistance | ( | 53 482 | 1015 |
| Dielectric strength 1 mm | kV/mm | 53 481 | 27 |
| Tracking resistance |
| 53 480 | KA 1 |
| Miscellaneous |
|  | Moisture absorption: Equilibrium in standard atmosphere (23 °C / 50 % relative humidity) | % | 53 714 | 0.2 |
| Water absorption at saturation at 23 °C | % | 53 495 | 0.36 |
| Resistance to hot water, washing soda |
|  | not resistant |
| Flammability |
| UL 94 | V2 |
| Resistance to weathering |
|  | not resistant |

* after storage in a standard 23/50 atmosphere (DIN 50 014) to equilibrium